Comparative Study on low temperature Bleaching and normal temperature bleaching on cotton fabric with peroxide

A

Dissertation submitted in the Partial Fulfilment of the requirement for the award   of the degree of

MASTER OF TECHNOLOGY IN TEXTILES

(Mid Term Evaluation)

(Maharshi Dayanand University, Rohtak)

Guided by:                                                                                                   Submitted By:

Dr.amit madhu                                                                                             Mahesh saini

The Technological Institute of Textile & Sciences, Bhiwani-127021

(2024-26)

CERTIFICATE

It is certified that the work presented in this dissertation Entitled that “comparative study of low temperature bleaching and normal temperature bleaching on cotton with peroxide”. For Textiles being submitted by Mr. Mahesh Saini to Maharshi Dayanand university, Rohtak for the award of the degree of masters of technology in textiles has been carried out under my guidance. The results reported in this dissertation have not been submitted in part or full to any university for the award of any degree or diploma.

Dr Amit Madhu

(Guide)

Assistant professor

Textile chemistry Department

T.I.T&S, Bhiwani

ACKNOWLEDGEMENT

It is true that every mission needs a spirit of dedication and hard work. But more than anything else, it requires appropriate guidance to reach the goal at right time.

No words can suffice my feelings of immense gratitude to my guide Dr Amit Madhu Head of Department T.I.T & S Bhiwani for his highly valuable and pains-taking guidance, unceasing encouragement, constructive criticism and parental affection during the course of this study. I am grateful to him for his precious time and intellect he devoted to bringing this work into its present form.it is indeed a matter of great pride for me that I have worked under the guidance of such able and noble teacher his involvement with originality has triggered and nourished the intellectual maturity that will help me for long time to come .I am proud to record that I had the opportunity to work with exceptionally experienced professor like him.

I would like to express my sincere thanks to Dr. Sanjay Pandya T.I.T.& S. Bhiwani for helping me in preparation of samples and experimental testing Profound thanks are due to all staff of T.I.T.& S Textile Chemical Processing Laboratory and Library of providing me required assistance during the course of this project

If would be an unpardonable mistake on my part if I don’t express my thanks to my classmates for their cooperation and good wishes during the entire period of my work.

Finally I feel my principal duty to express my deep regard profound sense of gratitude and heartful to my parents for their noble guidance invaluable advice and energetic inspiration to yield the present work as a successful piece of dissertation .

CONTENT

1.Introduction to bleaching

2.literature survey

3.mechanism of bleaching

4.chemistry of bleaching

5.standard test for preparatory process

6.Recent research work on Bleaching

7.Objective

8. Project plan

9. References

Introduction to Bleaching process in Textile Industry

Bleaching Process

Bleaching is an important process of wet processes in the textile industry. It is a pretreatment process of dyeing and printing which remove natural color from the fabric to get a bright white fabric. Bleaching is a process used in textile production to whiten fabrics. The bleaching process is done chemically in dyeing and printing textile mills. So the Bleaching process is a chemistry. This process also increased the absorbency capacity of fabrics. After completing the bleaching process, the grey fabric becomes very white and bright. scouring is the previous process of bleaching in the textile wet process. Then mercerizing process only before dying. This article is all about the chemistry of the bleaching process in the textile industry wet processes.

CHAPTER 2: LITERATURE REVIEW

2.1 Introduction

Bleaching is a crucial preparatory process in textile wet processing aimed at improving the whiteness and absorbency of fibers by removing natural coloring matter, waxes, and impurities. Conventional bleaching typically relies on strong oxidizing agents such as sodium hypochlorite (NaOCl) or hydrogen peroxide (H₂O₂) under alkaline conditions. However, these methods are associated with significant environmental and operational drawbacks, including high energy consumption, high chemical usage, and the generation of toxic effluents.

In recent decades, the textile industry has shifted its focus toward sustainable and eco-friendly bleaching technologies that minimize environmental pollution, reduce water and energy usage, and maintain fabric quality. This chapter reviews the existing literature on conventional bleaching methods, emerging eco-friendly bleaching agents, enzyme-assisted bleaching, plasma and ozone treatments, and other innovative sustainable alternatives.

2.2 Conventional Bleaching Methods

2.2.1 Sodium Hypochlorite Bleaching

Historically, sodium hypochlorite has been a common bleaching agent due to its strong oxidizing ability and cost-effectiveness (Karmakar, 1999). However, the use of hypochlorite leads to the formation of adsorbable organic halides (AOX), which are toxic and non-biodegradable. These byproducts pose severe environmental hazards, leading to strict regulations and a gradual decline in hypochlorite usage.

2.2.2 Hydrogen Peroxide Bleaching

Hydrogen peroxide bleaching under alkaline conditions, typically stabilized with sodium silicate or magnesium salts, remains the most widely used method in modern textile industries. It offers a cleaner alternative to hypochlorite but still requires high temperatures (80–95 °C) and strong alkali (NaOH), resulting in energy-intensive processes and potential fiber damage (Sharma & Gupta, 2015). The decomposition of H₂O₂ into water and oxygen makes it relatively eco-friendly, but the high chemical load and effluent alkalinity remain major concerns.

2.3 Eco-Friendly Alternatives

2.3.1 Enzymatic Bleaching

Enzymes, especially laccases, peroxidases, and cellulases, have emerged as promising eco-friendly bleaching agents.

- Laccase-assisted bleaching utilizes the oxidative power of laccase enzymes (EC 1.10.3.2) in the presence of mediators such as violuric acid or TEMPO to degrade natural pigments in cotton (Abadulla et al., 2000).

- Catalase treatment can be applied post-bleaching to decompose residual hydrogen peroxide into water and oxygen, minimizing rinsing requirements (Tzanov et al., 2001).

- Enzymatic bleaching operates under mild conditions (pH 5–8, 40–60 °C), leading to significant savings in energy and water and preserving fiber integrity.

Recent studies by Zille et al. (2015) have shown that enzyme-assisted bleaching combined with ultrasound can further enhance whiteness and reduce processing time. However, the higher cost of enzymes and their sensitivity to temperature and pH are still limiting factors for industrial adoption.

2.3.2 Ozone Bleaching

Ozone (O₃) is a strong oxidizing agent that decomposes into oxygen without leaving harmful residues, making it a highly eco-friendly bleaching medium.

- Ozone bleaching at room temperature offers substantial reductions in water and energy use.

- Studies (Perincek et al., 2008) demonstrated that ozone treatment in a moist atmosphere effectively removes natural pigments from cotton while maintaining tensile strength.

- The main challenges include the need for specialized ozone-resistant equipment and ensuring uniform ozone distribution for consistent bleaching.

Ozone bleaching has been found particularly suitable for denim desizing and decolorization and as a pretreatment for peroxide bleaching to reduce chemical consumption (Ahn et al., 2011).

2.3.3 Plasma Treatment

Plasma technology, especially low-temperature atmospheric plasma, modifies the fiber surface through physical and chemical interactions without using water or chemicals.

- It enhances the hydrophilicity of cotton and improves the subsequent uptake of bleaching agents (Shishoo, 2007).

- Plasma treatment introduces oxygen-containing functional groups on the fiber surface, facilitating oxidation of chromophoric compounds.
Although plasma treatment alone does not achieve full whiteness, it is often combined with mild peroxide or enzymatic bleaching for synergistic effects.

2.3.4 Activated Hydrogen Peroxide Systems

Recent research focuses on the activation of H₂O₂ using catalysts or alternative energy sources to lower temperature and time requirements.

- Ultrasound, microwave irradiation, and UV activation of peroxide enhance the formation of hydroxyl radicals, leading to faster bleaching at lower temperatures (Mahapatra et al., 2018).

- Peracetic acid and TAED (tetraacetylethylenediamine) are also used as activators for low-temperature bleaching. These approaches result in improved fabric quality and lower environmental footprint.

2.3.5 Biobleaching Using Microbial Cultures

Microbial biobleaching involves the use of fungi or bacteria capable of secreting oxidative enzymes such as lignin peroxidase or manganese peroxidase.

- White-rot fungi (e.g., Phanerochaete chrysosporium) have shown potential in decolorizing natural pigments in cotton and jute (Gulrajani et al., 2012).

- This method is particularly advantageous for cellulosic and lignin-rich fibers, reducing chemical oxygen demand (COD) in effluents by up to 60%.
However, the process control and reproducibility in large-scale operations remain challenges.

2.4 Comparative Assessment of Eco-Friendly Methods

| Bleaching Method | Temperature (°C) | Environmental Impact | Fabric Strength | Whiteness Index | Feasibility |
| --- | --- | --- | --- | --- | --- |
| Conventional H₂O₂ | 80–95 | Moderate effluent load | Moderate loss | High | Widely used |
| Enzymatic | 40–60 | Very low | Excellent | Moderate–High | Costly enzymes |
| Ozone | 25–40 | Very low | Excellent | Moderate | Equipment cost |
| Plasma | 25–30 | Negligible | Excellent | Moderate | High setup cost |
| Activated H₂O₂ | 50–60 | Low | Good | High | Scalable |

2.5 Research Gaps

While numerous eco-friendly bleaching techniques have been investigated, challenges persist in their industrial scalability, cost efficiency, and reproducibility. Enzyme-based and plasma-assisted bleaching show promise for future adoption but require optimization for continuous processing systems. Integrating hybrid processes, such as enzyme–ozone or plasma–peroxide combinations, may offer the best balance between sustainability and performance.

Low-Temperature Bleaching

Low-Temperature Bleaching (LTB) is an eco-friendly textile treatment that uses hydrogen peroxide activated by special chemicals (activators) at lower temperatures (around 60-80°C) to achieve whiteness, reducing energy consumption and fabric damage compared to traditional high-heat methods. Key activators include TAED (tetraacetylethylenediamine) or surfactants, allowing for better whiteness with less weight loss, but sometimes requiring more chemicals and careful post-treatment.

How it Works

- Activators: Instead of relying on high heat to break down hydrogen peroxide, LTB uses activators like TAED or specialized surfactants (e.g., OPTAVON LTB) to generate peracetic acid in situ, which bleaches effectively at lower temperatures.

- Conditions: Temperatures are typically maintained between 50°C and 80°C, with times varying from 20 to 60 minutes, depending on the activator and fabric.

- Chemicals: Besides activators, formulas often include sodium silicate, sodium hydroxide, sequestering agents (to bind metal ions), and detergents.

Benefits

- Energy Savings: Lower temperatures significantly cut down energy costs.

- Fabric Preservation: Reduced thermal stress means less fabric weight loss and better retention of hydrophobic substances, improving fabric value and feel.

- Environmental: Lower energy use and less substance removal lead to less chemical oxygen demand (COD) in wastewater.

- Dyeing Performance: Achieves excellent whiteness for subsequent dyeing, with good dye uptake and colorfastness.

Considerations

- Chemical Usage: May require higher quantities of alkali, peroxide, and other auxiliaries compared to conventional methods.

- Post-Treatment: Requires thorough washing (antiperoxidase process) to remove residual chemicals for optimal dyeing.

Example Process (Typical)

- Preparation: Mix water, hydrogen peroxide, activator (like TAED or surfactant), alkali, and stabilizers.

- Treatment: Introduce cotton fabric and heat to around 60°C for an hour.

- Washing: Wash with hot and cold water.

- Drying & Testing: Dry and measure whiteness index (CIE method).

MECHANISM OF BLEACHING OF TEXTILE

The mechanism of textile bleaching

involves the chemical alteration or destruction of natural coloring matters (chromophores) in the fibers, primarily through oxidation reactions. These reactions use specific chemical agents to break the double bonds within the conjugated systems of the pigment molecules, rendering them colorless.

The two main types of chemical bleaching are oxidative and reductive bleaching, each employing different agents and mechanisms.

Oxidative Bleaching

This is the most common method, especially for natural fibers like cotton, and uses agents that release active oxygen or chlorine species.

.

  - Characteristics: It is considered a universal and environmentally friendly bleaching agent as its byproducts are water and oxygen. Stabilizers, such as sodium silicate, are used to control its rapid decomposition and ensure a uniform bleaching action while minimizing fiber damage.

- Sodium Hypochlorite

The hypochlorous acid further dissociates to produce active oxygen, which then oxidizes the coloring matter. The hypochlorite ion itself is also responsible for the bleaching action.

  - Characteristics: It is a strong and economical bleaching agent, historically the oldest industrial method for cotton. However, it is being used less due to environmental concerns over the formation of absorbable organic halogens (AOX) and the risk of fiber degradation if not carefully controlled for pH and temperature.

Reductive Bleaching

This method is used for specific synthetic fibers (like polyamides and polyacrylates) and some animal fibers (like wool and silk).

- Mechanism: Reducing agents, such as sodium hydrosulphite, convert the double bonds within the chromophore into single bonds by adding hydrogen, which eliminates their ability to absorb visible light.

- Characteristics: The whiteness produced by reductive bleaching may not be permanent and can revert to the original color upon exposure to air (re-oxidation).

The key mechanism across all types involves the chemical attack on the chromophores (color-producing parts of molecules), changing their structure so they no longer reflect visible light as color. The result is a white or colorless material, which may be further enhanced with optical brightening agents (OBAs) to achieve a brilliant white appearance.

STRATEGY FOR BLEACHING OF TEXTILE

An effective textile bleaching strategy involves

selecting the appropriate bleaching agent based on the fiber type, performing necessary pre-treatment and post-treatment steps, and controlling process parameters like pH, temperature, and time to achieve the desired whiteness with minimal fiber damage and environmental impact.

Key Process Steps

The general strategy for textile bleaching involves several stages to ensure effective impurity removal and a quality finish:

- Pre-treatment (Scouring & Desizing): Raw "greige" fabric contains natural impurities (waxes, pectins, proteins, natural pigments) and manufacturing residues (sizing agents, lubricants). Scouring removes these substances, making the fabric more hydrophilic and ensuring uniform bleaching. This step can be combined with bleaching in modern processes.

- Bleaching: This primary step uses chemicals to destroy the natural coloring matter (chromophores) in the fibers, resulting in a white or color-neutral base.

- Neutralization/Clean-up: After bleaching, residual chemicals must be removed or neutralized to stop the bleaching action and prevent damage to the fiber or interference with subsequent dyeing.

- Optical Brightening (Optional): Optical brightening agents (OBAs) may be applied to enhance the material's brightness by reflecting blue light, making it appear a more brilliant white.

sed for synthetic fibers (polyamide, polyester/cotton blends) and bast fibers like flax due to its high whiteness potential and low fiber damage. It is activated in acidic conditions (pH 3.5–4) but requires corrosion inhibitors for equipment and careful handling to manage chlorine dioxide gas evolution.

- Reductive Bleaches: Agents like sodium hydrosulfite (sodium dithionite) are used for fibers such as polyester and nylon, where an oxidative bleach might be ineffective or damaging. The whiteness produced is, however, not always permanent.

- Eco-Friendly Options (Enzymatic & Ozone): Emerging sustainable methods use natural enzymes (like pectinases and laccases) or ozone gas. These methods reduce water and energy consumption and generate less harmful effluent, preserving fiber integrity.

Operational and Safety Considerations

- Process Control: Maintaining precise pH, temperature, and concentration is critical to ensure optimal bleaching efficacy while minimizing damage to the textile fibers.

- Safety: Use of personal protective equipment (PPE) and ensuring proper ventilation are essential when handling industrial bleaching chemicals. Never mix chlorine bleach with acids or ammonia, as this creates toxic fumes.

- Effluent Treatment: Bleaching wastewater must be neutralized and treated to remove harmful residues (e.g., residual hydrogen peroxide is often neutralized using the enzyme catalase) before discharge to minimize environmental impact.

CHEMISTRY OF BLEACHING OF TEXTILE

The chemistry of textile bleaching involves

using The process relies on breaking the chemical bonds (typically conjugated double bonds) responsible for the color.

Bleaching agents change the color-absorbing properties of the chromophores:

oxidizing or reducing agents to decolorize the natural pigments (chromophores) in fibers, making the fabric white and increasing its absorbency for subsequent dyeing or printing.

Post-Bleaching Steps

After chemical treatment, the fabric is thoroughly washed and neutralized (e.g., using an anti-chlorine treatment after hypochlorite bleaching) to remove residual agents that could interfere with dyeing or damage the fabric over time. Optical Brightening Agents (OBAs), which absorb UV light and re-emit blue light, are often applied to achieve a brilliant "market white" finish.

Textile bleaching chemistry involves using oxidative (like hydrogen peroxide, hypochlorite) or reductive (like sodium hydrosulphite) agents to destroy the chromophores (color bodies) in fibers, which are typically organic compounds with conjugated double bonds. Oxidative agents break these bonds, making the color molecules colorless, while reductive agents convert double bonds to single bonds, eliminating light absorption, suitable for different fiber types (cellulosics vs. synthetics). Key factors like pH, temperature, and stabilizers control the reaction to achieve whiteness while minimizing fiber damage.

Oxidative Bleaching (Most Common)

- Mechanism: The bleaching agent decomposes to form highly reactive oxygen species (like the perhydroxyl ion,

HO2-

𝐻𝑂−2

), which attack and break the conjugated double bonds within the chromophore molecules, rendering them colorless.

- Agents:

  - Hydrogen Peroxide (H₂O₂): Most popular for cotton/cellulosics. Works best with alkali (like NaOH) at pH 10-11 to generate the active perhydroxyl ion, requiring stabilizers (silicates, EDTA) to prevent rapid decomposition and fiber damage.

  - Sodium Hypochlorite (NaClO): Older, effective but harsher; requires careful pH and temperature control (pH 9-11, <30°C) to prevent cellulose damage.

  - Chlorine Dioxide (ClO₂): Generated from sodium chlorite (NaClO₂), effective for various fibers with low damage.

- Process: Often combined with scouring and desizing, using alkaline conditions and heat (80-100°C) for cotton.

Reductive Bleaching

- Mechanism: Converts colored compounds by adding hydrogen, changing double bonds to single bonds, thus removing color.

- Agents:

  - Sodium Hydrosulphite (Sodium Dithionite, Na₂S₂O₄): A powerful reducing agent.

- Application: Used for fibers like polyamides, acrylics, and polyacetates that are sensitive to oxidation.

Key Factors & Control

- pH: Crucial for activating agents like H₂O₂ (alkaline) or controlling ClO₂ (acidic).

- Temperature: Affects reaction rate; too high with H₂O₂ or hypochlorite can damage fibers.

- Stabilizers: Manage decomposition of H₂O₂, preventing fiber degradation.

- Clean-up: Thorough rinsing after bleaching removes residual agents to ensure even dyeing later.

CONVENTIONAL TEXTILE BLEACHING VERSES ADVANCE BLEACHING METHOD

Conventional textile bleaching uses harsh chemicals like sodium hypochlorite or high concentrations of hydrogen peroxide at high temperatures, requiring extensive water and energy

. Advanced bleaching methods, such as enzymatic and ozone bleaching, are more sustainable, operating at lower temperatures with reduced resource consumption and less fiber damage.

Conventional Textile Bleaching

The traditional method, primarily using an alkaline hydrogen peroxide or sodium hypochlorite bath, effectively removes natural color impurities but comes with significant drawbacks.

- Chemicals Used: High concentrations of chemicals, including hydrogen peroxide, sodium hypochlorite, stabilizers, and sodium hydroxide, are used to achieve a desired whiteness.

- Process Conditions: The process is energy-intensive, requiring high temperatures (often near boiling, around 98 °C) and long reaction times (up to 90 minutes).

- Environmental Impact: It consumes large amounts of water for extensive rinsing cycles and produces high volumes of effluent with high chemical oxygen demand (COD), total suspended solids (TSS), and persistent color, posing environmental risks.

- Fabric Quality: The aggressive chemical reactions can lead to fiber weakening, reducing fabric tensile strength and durability.

Advanced Bleaching Methods

Advanced methods focus on sustainability and improved fabric quality while achieving comparable or superior whiteness. These technologies often leverage biological catalysts or physical processes.

| Method | Key Features | Advantages | Challenges |
| --- | --- | --- | --- |
| Enzymatic Bleaching | Uses biodegradable enzymes (e.g., pectinase, laccase) as catalysts. | Operates at lower temperatures (40–60 °C), is eco-friendly, reduces chemical use, and results in less fiber damage, preserving fabric strength. | Requires precise control of pH and temperature, may involve higher initial investment, and might need longer reaction times. |
| Ozone Bleaching | Uses oxygen-derived gas (ozone) to oxidize impurities. | Significantly reduces water usage (up to 50%) and operates at lower temperatures (around 35 °C), offering substantial energy savings. | Requires specialized equipment and controlled conditions to prevent over-oxidation of the fabric. |
| UV-Assisted Bleaching | Employs ultraviolet (UV) radiation instead of a heated bath. | Highly energy-efficient, operates at room temperature, and minimizes wastewater effluent due to direct application on fabric. | Still emerging and faces scalability challenges. |
| Electrochemical Bleaching | Generates powerful, controlled bleaching agents (like sodium hypochlorite) from an electrolytic cell on-site. | Eliminates effluent transport problems, offers high control and reliability, and is generally cleaner. | Requires specialized electrochemical equipment. |
| Low-Temperature Peroxide Bleaching | Uses activators (e.g., potassium persulfate) to make hydrogen peroxide effective at lower temperatures. | Requires less energy and water, is eco-friendly, and causes less weight loss and tensile strength reduction compared to the conventional hot peroxide process. | Can have a slightly lower whiteness index compared to high-temperature conventional methods. |

The shift towards advanced methods is driven by the textile industry's growing need for sustainable and efficient processes that reduce environmental impact without compromising product quality.

PERFORMANCE TEST FOR BLEACHING OF TEXTILE

The performance of textile bleaching is evaluated by assessing several key properties of the fabric before and after the process. The main tests measure the desired aesthetic outcome (whiteness) and any potential damage to the fiber's integrity

.

The most common performance tests include:

Whiteness and Color Measurements

The primary goal of bleaching is to achieve a high degree of whiteness or a uniform base for subsequent dyeing.

- Whiteness Index (WI) and Yellowness Index: These are instrumental analyses performed using a spectrophotometer (e.g., in accordance with ASTM E313 standards). The results are often expressed using scales like the Berger whiteness scale or CIE whiteness degree.

- Color Strength (K/S value): This value, calculated using the Kubelka-Munk equation, helps assess the effectiveness of color removal and the fabric's ability to be dyed uniformly afterward.

Mechanical Strength Tests

A good bleaching process removes impurities without significantly degrading the cellulose fibers. Mechanical strength tests ensure the fabric remains durable enough for its intended end-use.

- Tensile Strength: This measures the force required to break a fabric sample under tension. Standards like ISO 13934-2:2014 are used for this test.

- Tear Strength: This test measures the fabric's resistance to tearing.

- Bursting Strength: This measures the resistance of knitted fabrics to rupture when force is applied perpendicular to the fabric plane (e.g., using a test machine that conforms to ISO 13938-2:1999 standards).

Physical and Chemical Analysis

These tests evaluate other important physical properties and residual chemical content.

- Weight Loss: The percentage of weight lost during the process indicates the amount of non-cellulosic impurities (like pectin, waxes, and natural coloring matter) that were successfully removed.

- Hydrophilicity/Absorbency: An effective bleaching process improves the fabric's ability to absorb water (wettability), which is crucial for uniform dyeing and finishing. Tests include the water drop test (AATCC Test Method 79-2007) and the capillary rise method.

- Residual Peroxide/Alkali Content: Chemical tests (e.g., using indicator paper strips or titration) are performed after bleaching and rinsing to ensure that no residual components remain in the fabric, which could interfere with subsequent processes or damage the fiber over time.

- pH Measurement: The pH of the fabric or process bath is checked to ensure it falls within a specified range, as extreme pH can cause fiber damage (e.g., hydrogen peroxide is most stable and effective in an alkaline environment)

Recent Research Work on Bleaching of Textile

Recent research on textile bleaching is primarily focused on developing eco-friendly, low-temperature and low- energy methods that reduce water consumption and minimize fiber damage compared to conventional high temperature hydrogen peroxide processes.                                          Key areas of research include:

Sustainable bleaching technologies

. Enzymatic Bleaching: This approach used enzymes such as pectinases and laccases to break down non-celluiosic impurities (like pectins, waxes, and natural pigments) add milder temperatures(40-60  )and neutral pH levels. This reduces the need for harsh chemicals, energy, and results in less fiber damage and lower effluent toxitcity (COD ,TDS, TSS) compared to traditional methods.

.Nano-Catalyzed and Photo-Bleaching: Researchers have developed photocatalytic systems using nanoparticles like titanium dioxide to achieve high whiteness under UV-A light at lower temperatures (e.g.,60 ).These methods activate bleaching agents (likeH)more efficiently, leading to reduced chemical usage, energy consumption, environmental impact while maintaining or surpassing conventional whiteness levels

. Low Temperature Activators: The use of organic or bio-based activators, such as tetraacetylethylenediamine (TAED), triacetin, peracetic acid, and sucrose octaacetate (SOA), Allows for effective hydrogen peroxide bleaching at lower temperature. This innovation significantly cut energy consumption (by up to 35-40%) and water usage while preserving fabric strength

. Ozone and plasma treatments: Ozone, gas and plasma technologies are being explored as highly sustainable, water-free or low water methods for oxidizing impurities. These methods offer significant reduction in chemical usage and wastewater generation. Though challenges in scalability and equipment costs remain a focus of current research.

. Electrochemical bleaching: This process involves generating sodium hydrochloride in Situ within an electrolytic cell using only salt and water. This method eliminates the need for transporting and storing hazardous chemical significantly reduce process time and produces no effluent problem, making it an eco-friendly alternative with improved whiteness index results.

. Process optimization and integration.

A significant trend is the development of one-step scouring and bleaching processes to save time, water and energy, often utilizing the aforementioned eco-friendly agent and techniques like ultrasound or UV assistance.

Overall, recent research underscores the textile industry’s transition towards sustainable. Practices, driven by stringent environmental regulation and  Consumer demand for eco-friendly product.

Recent research textile bleaching focuses heavily on developing

Sustainable, low-temperature, and energy-efficient alternatives to conventional high-temperature hydrogen peroxide method. key areas of innovation include enzymatic, photocatalytic and activator-assisted processes that reduce environmental impact and preserve fabric integrity

. Key Research Areas and Innovations

. Enzymatic bleaching this method used bio catalysts like pectinases and laccases To selectively break down non-cellulosic impurities (pectins, waxes, etc.) Add milder temperature and natural PH level (40-60   pH5-7). This approach significantly reduces energy and water consumption and minimizes fiber damage Compared to conventional methods.

. Nano-catalyzed and photo Bleaching: Researchers have developed photocatalytic systems using nanoparticles such as. Such as titanium. Dioxide(Ti Doped with single bowl carbon. Nanotube. To enhance bleaching differentially using. UVA Light. These method can achieve high wildness indices at low temperature. Around 60 degrees Celsius. Saving substantial energy and water while producing less waste.

Objectives

The main objectives of the work are.

1.To minimise the pin holes issue in shirting qualities like 60 X60, poplin, plain weave more than 40 count.

2.To analyse the Performance effect in dyeing.

3.To Evaluate absorbancy, whiteness, tegwa.

4.To collect the grey sample, bleach sample,dyed samples of low temperature bleaching and normal temperature bleaching.

5.To evaluate the utility cost, chemical cost in comparison to low temperature and normal temperature.

Project plan

The plan executed to achieve the objective of this work is depicted below;

Literature survey

Sampling for individual application of peroxide bleaching at normal temperature and low temperature

Collection of samples

Evalution of pin holes

Comparative evaluation of samples

Comparative study with  respect to utility cost,chemical cost

Performance effect in dyeing

References

- Karmakar, S. R. Chemical Technology in the Pre-treatment Processes of Textiles. Elsevier, 1999.

- Abadulla, E., Tzanov, T., Costa, S. A., Robra, K. H., Cavaco-Paulo, A., & Gübitz, G. M. (2000). Decolorization and bleaching of cotton by laccase mediator system. Applied and Environmental Microbiology, 66(8), 3357–3362.

- Tzanov, T., Cavaco-Paulo, A., Gubitz, G. M. (2001). Catalase effect on hydrogen peroxide bleaching of cotton. Textile Research Journal, 71(5), 394–399.

- Perincek, S., Bahtiyari, M. I., & Eren, H. A. (2008). Ozone bleaching of cotton fabrics. Ozone: Science & Engineering, 30(3), 204–209.

- Ahn, Y. S., Lee, Y. S., Kim, H. S. (2011). Ozone-based bleaching for textile fibers. Textile Research Journal, 81(10), 1012–1019.

- Shishoo, R. (Ed.). Plasma Technologies for Textiles. Woodhead Publishing, 2007.

- Gulrajani, M. L., Gupta, D., & Kumar, V. (2012). Microbial bleaching of cotton fabrics. Indian Journal of Fibre & Textile Research, 37, 246–252.

- Mahapatra, N. N., et al. (2018). Low-temperature bleaching using activated hydrogen peroxide systems. Journal of Cleaner Production, 175, 104–112.

- Zille, A., Oliveira, F., & Souto, A. P. (2015). Ultrasound-enhanced enzymatic bleaching of cotton. Carbohydrate Polymers, 123, 329–336.

- Sharma, A., & Gupta, D. (2015). Environmentally friendly bleaching processes for textiles. Textile Progress, 47(1), 1–45.